Production Name:   Polyaspartic acid Sodium salt（PASP）

CERTIFICATE OF ANALYSIS

| Testing Criterion |  | Q/01XT0101-2021 |  |  |  | Batch Number |  |  | 20230810010101 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Manufacturing date |  | Aug. 10, 2023 |  |  |  | Expiry Date |  |  | Aug.10, 2024 |  |
| Quantity |  | 5.0MT |  |  |  |  |  |  |  |  |
| Inspection Item |  |  |  | Indication Range |  |  |  | Check Result |  |  |
| Appearance |  |  |  | Yellow to Reddish-brown Clear Solution |  |  |  | Reddish-brown Clear Solution |  |  |
| Solid Content % |  |  |  | ≥40.0 |  |  |  | 40.62 |  |  |
| Density g/cm3 (20℃) |  |  |  | ≥1.22 |  |  |  | 1.25 |  |  |
| Limiting Viscosity dl/g(30℃) |  |  |  | 0.055-0.090 |  |  |  | 0.056 |  |  |
| PH(10g/l in solution) |  |  |  | 8.5-10.5 |  |  |  | 9.3 |  |  |
| Conclusion： Qualified |  |  |  |  |  |  |  |  |  |  |
| Inspector | Hao Lina |  | Audit |  | Cui Xiaoming |  | Date |  |  | Aug. 10, 2023 |